Appendix A:

The following information on cartilage mechanical testing was extracted from literature to provide a summary of selected studies with varied goals and objectives.

Table A1: Specimen summary of selected studies focused on articular cartilage mechanical characterization.

Study	Goal	Specimen source	Specimen source	Specimen age / and/or gender	# of specimens and/or samples
Langelier et. al., 1	Assess strain and strain rate dependent stiffness and subsequent compression response	Bovine	Bovine	Gender: Not reported / Age: 1-2 yr old	Samples: 4 discs/speed
Toyras et. al., 2	Determine Young's modulus and thickness	Bovine	Bovine	Gender: Not reported / Age: Not reported	Specimens: 7
Lai et. al., 3	Investigate depth varying compressive strains	Bovine	Bovine	Gender: Not reported / Age: Young	Specimens: 6 / Samples: 72
Boschetti et. al., 4	Properties of cartilage under compression	Human	Human	Gender: 2 males, 1 female / Age: 73-M, 75-M, 81-F	Specimens: 3 / Samples: 33 discs
Jurvelin et; al., 5	Mechanical anisotropy of knee cartilage	Human	Human	Gender: 3 females, 7 males / Age: 23- 50 yrs	Specimens: 10 / Samples: 20
Treppo et. al., 6	Biomechanical comparison of knee-ankle cartilage pairs	Human	Human	Gender: Not reported / Age: 14, 22, 38 yrs (both left and right), 31, 45 yrs (only left)	Specimens: 8 / Samples: 10 from each tibiofemoral joint, 4 from each ankle joint.
Armstrong et. al., 7	Variation in properties with age, water content, degeneration	Human	Human	Gender: Not reported / Age: 56.4 yrs (SD: 19.13)	Specimens: 103 / Samples: 103
Charlebois et al., 8	Age and depth dependent tensile properties	Bovine	Bovine	Gender: Not reported / Age: < 12 months (n=9), between 12 and 24 months (n =11), over 24 months (n=6).	Specimens: 26
Froimson et al., 9	Cartilage surface fibrilation effects	Human	Human	Gender: / Age:18-41 yrs	Specimens: 17 / Samples: 10 sites / specimen
Bellucci et al., 10	Articular cartilage under cyclic tensile load	Human	Human	Gender: Not reported / Age: 48 yrs	Specimens: 1 / Samples: 72
Gao et al., 11	Depth and rate dependent cartilage behavior	Porcine	Porcine	Gender: Not reported / Age: 8 months	Specimens:1 / Samples: 18
Changoor et al., 12	Effects of freezing	Bovine	Bovine	Gender: / Age: ~ 6 months	Specimens: 1 / Samples: 8 sites/ 4 samples each
Thambyah et al., 13	Properties of cartilage covered by meniscus	Human	Human	Gender: male / Age: 62-70 yrs	Specimens: 7 / Samples: number of locations not specified
Bursac et al., 14	Assess confined and unconfined stress relaxation with transversely isotropic model	Bovine	Bovine	Gender: Not reported / Age: 3-4 weeks old	Specimens: 3 / Samples: 9
Nguyen et al., 15	Swelling influences on cartilage mechanics in compression and shear	Bovine	Bovine	Gender: Not reported / Age: Immature (details not provided)	Specimens: 7 / Samples: 50
G. E. Kempson 16	Relationship between tensile properties and age	Human	Human	Gender: Not reported / Age: 8-91 yrs	Specimens: 24 / Samples: not reported
Athanasiou et al., 17	Inter-species comparison of mechanical properties	Human and other	Human and other	Gender: Not reported / Age: 24, 35, 43 yrs- human. Others young adults.	Specimens: total 34 / Samples: 3 locations / specimen
Robinson et al., 18	Normal vs osteoarthritic (OA) cartilage	Human	Human	Gender: 10 specimens OA (4 male,6 female), 3 specimens normal (1 male, 2 female) / Age: 69.7± 9.3 yrs (OA), 59.1 ±7.2 yrs (normal)	Specimens: 13 / Samples: 51 OA, 43 normal
Deneweth et al., 19	Tibial plateau heterogeneity	Human	Human	Gender: Female / Age: 18-55 yrs	Specimens: 8 / Samples: 21/ specimen
Korhonen et al., 20	Equilibrium response at confined, unconfined compression and indentation	Bovine	Bovine	Gender: Not reported / Age: Not reported	Specimens: 1 / Samples: 26
Shepherd et al., 21	Instantaneous compressive modulus	Human	Human	Gender: 3 male, 8 female / Age: 65.1 (14.3) yrs.	Specimens: 11 sets / Samples: 75 sites on each knee, 50 on each hip and 35 on each ankle
Nissi et al., 22	Estimation of mechanical properties using MRI	Human, bovine, porcine	Human and other	Gender: Not reported / Age: 24-78 yrs (human), 1-3 yrs (bovine), 4 months(porcine)	Specimens: 12 (human), 12 (bovine), 11 (porcine) / Samples: not reported
Morel et al, 23	Study effects of injurious compression	Bovine	Bovine	Gender: Not reported / Age: 18 month old	Specimens: 1 / Samples: 55

Table A2: Sample preparation details for studies listed in table A1.
Study	Goal	Sample dimensions, method of dimension measurement	Sample preparation / (Previously frozen, hydrated, temperature, stabilized before testing)
Langelier et. al.,	Assess strain and strain rate dependent stiffness and subsequent compression response	3 mm disc, varying thickness (<1mm) / Measured using: microscope	Method of sample extraction/ preparation: orthopedic coring bit / Previously frozen: not reported / Hydrated: yes / Hydration source: Hank’s balanced salt solution (HBSS) with protease inhibitors / Temperature: ambient / Stabilization: HBSS with antibiotics and protease inhibitors at 4°C (36 Hrs maximum)
Toyras et. al.,	Determine Young's modulus and thickness	For unconfined compression: 3 mm diameter, for indentation: spherical-ended indenter (diameter: 0.500 mm, height: 0.100 mm), / Measured using: reference material testing device (unconfined compression) / based on constant sound velocity, 1654 m/s (ultrasound)	Method of sample extraction / preparation: not reported / Previously frozen: no / Hydrated: yes / Hydration source: Physiological saline / Temperature: not reported / Stabilization: not reported
Lai et. al.,	Investigate depth varying compressive strains	4 mm diameter / 1500 μM thick (bottom removed) / Measure using: not reported. Strain measurement (inverted fluorescence microscope)	Method of sample extraction / preparation: 6 mm biopsy punch, 4 mm samples punched before testing, slcied using sliding microtome / Previously frozen: Yes / Hydrated: yes / Hydration source: Phosphate buffered saline (PBS) with protease inhibitors / Temperature: Not reported / Stabilization: PBS (testing, ) treated with 1 μm ethidium homodimer-1 (EthD-1, Invitrogen, Carlsbad, CA) in PBS for 3 h at room temperature (for imaging)
Boschetti et. al.,	Properties of cartilage under compression	5 mm diameter, 650 micron thick, 3 layers / Measured using: stereomicroscope	Method of sample extraction / preparation: 9mm diameter bone and cartilage discs using a drill / Previously frozen: no, frozen after harvesting / Hydrated: yes / Hydration source: Phosphate buffered saline (PBS) with protease inhibitors / Temperature: ambient / Stabilization: Phosphate buffered saline with protease inhibitors
Jurvelin et; al.,	Mechanical anisotropy of knee cartilage	1.7 mm diameter, 1 mm thick / Measured using: light microscope	Method of sample extraction / preparation: 8mm diameter dermal biopsy punch, 1.7mm diameter samples punched normal and tangential to articular surface. / Previously frozen: no / Hydrated: Not reported / Hydration source: Not reported / Temperature: Not reported / Stabilization: Phosphate buffered saline (prior to testing)
Treppo et. al.,	Biomechanical comparison of knee-ankle cartilage pairs	3 mm diameter disc, top 1mm slices / Measured using: current sensing micrometer	Method of sample extraction/ preparation: 9 mm cores drilled first, 3mm cylindrical discs punched with dermal punch. / Previously frozen: Not reported / Hydrated: Not reported / Hydration source: Not reported / Temperature: Not reported / Stabilization: 0.1 M NaCl and 0.05 M Trizma buffer, pH 7.4. at -25°C
Armstrong et. al.,	Variation in properties with age, water content, degeneration	6.35 mm diameter / Measured using: microscope	Method of sample extraction/ preparation: according to method described by Lipshitz and Glimcher. / Previously frozen: yes / Hydrated: yes / Hydration source: Ringer’s solution / Temperature: ambient / Stabilization: Not reported
Charlebois et al.,	Age and depth dependent tensile properties	6-8 mm wide, 2 cm long, ~ 5-7 mm thick bone cartilage blocks. Tensile sample: 250 μm thick. / Measured using: micrometer	Method of sample extraction/ preparation: initial blocks obtained using cast-cutters. Tensile samples obtained using vibratome. / Previously frozen: No / Hydrated: Yes / Hydration source: Hank’s buffered saline solution (PBS) with 1% penstrep. / Temperature: Not reported / Stabilization: PBS/ penstrep
Froimson et al.,	Cartilage surface fibrilation effects	1.5 mm diameter indentor / Measured using: cartilage thickness measured using needle probe method	Method of sample extraction/ preparation: indentation, no extraction / Previously frozen: yes, until testing / Hydrated: Not reported / Hydration source: Not reported / Temperature: Not reported / Stabilization: Not reported
Bellucci et al.,	Articular cartilage under cyclic tensile load	0.2 mm thick, 1mm by 9 mm, multiple depths / Measured using: thickness measured using a custom built apparatus that uses electrical conductivity of cartilage.	Method of sample extraction/ preparation: 16 plugs harvested with a reamer / Previously frozen: frozen after sample extraction / Hydrated: yes / Hydration source: buffer solution / Temperature: ambient / Stabilization: not reported
Gao et al.,	Depth and rate dependent cartilage behavior	5.5 by 4 mm, 2 mm thick / Measured using: microscope	Method of sample extraction/ preparation: with a steel trephine / Previously frozen: Not reported / Hydrated: Not reported / Hydration source: Not reported / Temperature: ambient / Stabilization: not reported
Changoor et al.,	Effects of freezing	3 mm diameter / Measured using: upright digital calipers	Method of sample extraction/ preparation: mosaicplasty punch / Previously frozen: yes / Hydrated: yes / Hydration source: Phosphate buffered saline (PBS) / Temperature: Not reported / Stabilization: stored in individual humid chambers at 4°C for up to 24 h, immersed in PBS for 15 min before testing.
Thambyah et al.,	Properties of cartilage covered by meniscus	Load bearing and non load bearing regions / Measured using: cartilage thickness measured using needle penetration and recording load once needle reached subchondral bone	Method of sample extraction/ preparation: not reported / Previously frozen: yes / Hydrated: not reported / Hydration source: not reported / Temperature: not reported / Stabilization: not reported
Bursac et al.,	Assess confined and unconfined stress relaxation with transversely isotropic model	4.5 mm diameter, 3.5 mm thick / Measured using: not reported	Method of sample extraction/ preparation: full thickness, 7 mm diameter (method not reported). Sample preparation not reported / Previously frozen: yes (in phosphate buffered saline (PBS) with protease inhibitors (PI)) / Hydrated: yes / Hydration source: PBS and PI / Temperature: ambient / Stabilization: Thawed at room temperature in PBS and PI
Nguyen et al.,	Swelling influences on cartilage mechanics in compression and shear	4mm diameter, 2 mm thick mid-substance / Measured using: nor reported	Method of sample extraction/ preparation: 6 mm biopsy punch / Previously frozen: no. frozen after extraction until tested / Hydrated: Yes / Hydration source: Phosphate buffered saline and protease inhibitors (PBS + PI) / Temperature: 37 °C / Stabilization: samples equilibrated at 4 C for 4h in 0.1x, 0.5x, 1x, 2x, 10x PBS + PI (n=10/group)
G. E. Kempson	Relationship between tensile properties and age	3 mm by 0.5 mm, 200 micron thick / Measured using: not reported	Method of sample extraction/ preparation: not reported (pointed to previous studies) / Previously frozen: yes / Hydrated: yes / Hydration source: Ringer’s solution / Temperature: not reported / Stabilization: not reported
Athanasiou et al.,	Inter-species comparison of mechanical properties	1.5 mm diameter indentor / Measured using: cartilage thickness measured using a penetrating needle probe.	Method of sample extraction/ preparation: Not reported / Previously frozen: yes / Hydrated: yes / Hydration source: saline / Temperature: room temperature / Stabilization: thawed at room temperature for 1h in normal saline with enzymatic inhibitors.
Robinson et al.,	Normal vs osteoarthritic (OA) cartilage	3 mm diameter osteochondral plugs / Measured using: micro CT scanner	Method of sample extraction/ preparation: 5mm osteochondral plugs harvested using hand held coring tool. 3 mm cylindrical plugs extracted using dermal punch. Outer ring used for histology. / Previously frozen: not reported / Hydrated: yes / Hydration source: immersed in phosphate buffered saline (PBS) with protease inhibitors and refrigerated at 4°C. / Temperature: ambient / Stabilization: PBS + PI at room temperature for 30 min
Deneweth et al.,	Tibial plateau heterogeneity	4 mm diameter , 0.9 – 4.4 mm thick / Measured using: digital vernier calipers	Method of sample extraction/ preparation: 4 mm diameter round hole hand punch and scalpel / Previously frozen: yes / Hydrated: yes / Hydration source: Phosphate buffered saline (PBS) / Temperature: not reported / Stabilization: not reported
Korhonen et al.,	Equilibrium response at confined, unconfined compression and indentation	3.7 mm diameter for compression (13mm plugs: 2 indentation, 2 UC and 2 CC were performed) / Measured using: thickness measured using steriomicroscope	Method of sample extraction/ preparation: 13 mm osteochondral samples were drilled. / Previously frozen: yes / Hydrated: yes / Hydration source: Phosphate buffered saline (PBS) with enzyme inhibitors. / Temperature: not reported / Stabilization: not reported
Shepherd et al.,	Instantaneous compressive modulus	1.58 mm radius (noted from referenced study) / Measured using: not reported (referenced previous study for details)	Method of sample extraction/ preparation: indentation, details not reported (referenced previous study for details) / Previously frozen: yes / Hydrated: not reported / Hydration source: not reported / Temperature: not reported / Stabilization: not reported
Nissi et al.,	Estimation of mechanical properties using MRI	4 mm diameter, full thickness / Measured using: not reported	Method of sample extraction/ preparation: samples prepared by drilling 16 mm osteochondral plugs, separating 4mm diameter cartilage samples for testing. / Previously frozen: yes (in phosphate buffered saline with enzyme inhibitors and 5mM benzamide HCL) / Hydrated: not reported / Hydration source: not reported / Temperature: not reported / Stabilization: not reported
Morel et al,	Study effects of injurious compression	4mm diameter bone, 2.7 mm diameter cart plugs, full thickness / Measured using: microscope	Method of sample extraction / preparation: drilled / Previously frozen: no / Hydrated: yes / Hydration source: 10 ml Dulbecco’s modified eagle media (DMEM) / Temperature: ambient / Stabilization: incubated for 17 days in DMEM before testing

Table A3: Testing details for studies listed in table A1. Selected results are reported. UC: unconfined compression, CC: confined compression, I: indentation, UT: Uniaxial tension

Study	Goal	Test type	Protocol (Tare load, preconditioning, testing)	Output/ results/ material properties
Langelier et. al.	Assess strain and strain rate dependent stiffness and subsequent compression response	UC	Tare load: 6g / Preconditioning: not reported / Test: compression-hold-release (12.5; 25; 50; 100; 150; 200; 250; 300 μm) using 1 of 3 ramp speeds (0.5; 5; 50 mm/s), 10 min relaxation.	Equilibrium moduli of the first test ramp (12.5 mm): 0.40– 0.61 MPa for low strain rate compression, 0.30– 0.56 MPa for moderate strain rate (fresh and frozen specimens) compression and 0.33–0.56 MPa for high strain rate compression. / Peak stiffness showed sensitivity to strain rate.
Toyras et. al.	Determine Young's modulus and thickness	Ultrasound, I and UC	Tare load: Not reported / Preconditioning: Not reported / Test: Unconfined compression – step-wise stress relaxation. 5 steps, each 4% of cartilage thickness, speed 2 mm/s, relaxation time of 13 min between each step. The equilibrium stress-strain data in the linear range during the three last steps used to determine the equilibrium Young’s modulus. Instantaneous modulus obtained from fourth step.	Young's modulus: 0.1-1.6 MPa
Lai et. al.	Investigate depth varying compressive strains	UC	Tare load: Not reported / Preconditioning: Not reported / Test: compressed at 1 μm/s to 5, 10, 15, and 20% strain, relax for 20 min at each offset (to obtain equilibrium compressive modulus and local strain distribution).	Average equilibrium compressive modulus: 0.447 (0.363, 0.531) MPa Local strains decrease with depth.
Boschetti et. al.	Properties of cartilage under compression	CC, UC	Tare load: Not reported / Preconditioning: Not reported / Test: 15 kPa for 1800s	Confined: Average aggregate modulus (layers 1,2 and 3 respectively): 0.25, 0.38, 0.5 MPa. / Unconfined: Average Equilibrium modulus (layers 1,2 and 3 respectively): 0.24, 0.38,0.5 MPa
Jurvelin et; al.	Mechanical anisotropy of knee cartilage	CC, UC	Tare load: Not reported / Preconditioning: Not reported / Test: step 10 μm, 1 μm/s up to 20 % strain. Relaxation limit: < 0.1g /min	Aggregate modulus: 0.845±0.383 MPa (normal direction) / Young's modulus: 0.581±0.168 MPa (normal direction)
Treppo et. al.	Biomechanical comparison of knee-ankle cartilage pairs	CC	Tare load: Not reported / Preconditioning: Not reported / Test: Static compressive strain 5-10% up to 25 %.	Femur (n=48): Average aggregate modulus = ~ 0.6 MPa, Tibial plateau (n=31): ~ 0.5 MPa, Talar cartilage (n= 27): ~ 9MPa. / Dynamic stiffness, hydraulic permeability and electrokinetic coupling coefficient also calculated.
Armstrong et. al.	Variation in properties with age, water content, degeneration	Creep CC	Tare load: Not reported / Preconditioning: Not reported / Test: 0.1 MPa constant stress	Modulus: 0.79 MPa (0.36)
Charlebois et al.	Age and depth dependent tensile properties	UT	Tare load: Not reported / Preconditioning: Not reported / Test: 5 ramps of 2% strain up to 80 microns (6 μm/second). 5.5 hr, 6.6hr, 7.5hr, 8.5hr, 9.5hr, 10.5hr wait times after each step including initial offset. 48 hour long tests	Peak modulus for the last step: 10.1 (3.3) MPa for young (n=7), 18.7(5.9) MPa for adolescent (n=6), and 28.3(16.6) MPa for adult (n=6). Equilibrium modulus for the last step: -0.1 (0.5) MPa for young (n=7), 4.4 (2.6) MPa for adolescent (n=6), and 15.4(9.6) MPa for adult (n=6).
Froimson et al.	Cartilage surface fibrilation effects	Biphasic I	Tare load: Not reported / Preconditioning: Not reported / Test: Not described	Average aggregate modulus: 0.42 MPa (Patella) / 0.6 MPa (trochlear grove). / Poisson’s ratio and permeability also calculated.
Bellucci et al.	Articular cartilage under cyclic tensile load	Cyclic UT	Tare load: Not reported / Preconditioning: Not reported / Test: 1.5 – 3 MPa maximum stress	Cycles to failure: 20 to 1.5 * 10^6
Gao et al.	Depth and rate dependent cartilage behavior	Creep UC	Tare load: Not reported / Preconditioning: Not reported / Test: UC: stress rates 0.0045, 0.045, 0.225 MPa/s, Creep: constant compressive stress levels of 0.1, 0.5 and 1 MPa, creep time: 60 min	Young's modulus: / at 0.0045 MPa /s: 1.4-4.8 MPa (superficial – deep layer) / at 0.045 MPa /s: 2.5-6.5 MPa (superficial – deep layer) / Creep strain decreases with depth.
Changoor et al.	Effects of freezing	UC	Tare load: Not reported / Preconditioning: Not reported / Test: ramps of 2% strain applied at 0.4% strain/s, relax until the load decay was 0.01 g/min	refrigeration at 4 °C: fibril modulus, day 1: average 16.5 MPa (n=8), day 12: average 5MPa (n=4). / refrigeration at 4 °C: matrix modulus, day 1: average 0.7 MPa (n=8), day 12: ~0.05 MPa / Freezing at 20 °C: fibril modulus, day 1: average 14 MPa (n=8), day 12: average 15 MPa (n=8). / Freezing at 20 °C: matrix modulus, day 1: average 0.5 MPa (n=8), day 12: average 0.45 MPa (n=8)
Thambyah et al.	Properties of cartilage covered by meniscus	I	Tare load: Not reported / Preconditioning: Not reported / Test: axial compression at a constant load of 0.5 N (0.6 MPa ), with the use of a 1-mm diameter indenter, 60s hold.	Lateral plateau not covered by meniscus: 2.13 (0.74) MPa / Medial plateau not covered by meniscus: 3.51 (1.42) MPa / Lateral plateau covered by meniscus: 3.77 (1.25) MPa / Medial plateau covered by meniscus: 5.13 (1.91) MPa
Bursac et al.	Assess confined and unconfined stress relaxation with transversely isotropic model	CC, UC	Tare load: ~ 3% ramp-strain / Preconditioning: Not reported / Test: Steps of 3% ramp up to 15 % strain (0.115 μm /s)	Aggregate modulus, MPa at 6%,9%,12%,15% strain: 1.72 (0.72), 1.23 (0.4), 0.97 (0.2), 0.79 (0.12). / Young's modulus, MPa at 6%,9%,12%,15% strain: 1.5 (0.5), 1.09 (0.43), 0.74 (0.28), 0.68 (0.13).
Nguyen et al.	Swelling influences on cartilage mechanics in compression and shear	UC	Tare load: Not reported / Preconditioning: Not reported / Test: 5%, 10%, 15%, and 20% strain at 0.1%/s, 20 min relaxation	For 1x PBS concentration, Equilibrium modulus: 1.47 ± 0.13 MPa / (moduli decreased with increased PBS concentration)
G. E. Kempson	Relationship between tensile properties and age	UT	Tare load: Not reported / Preconditioning: Not reported / Test: constant rate of extension of 5 mm/min. Tensile stiffness determined from the gradient to the stress strain curve at 2 levels of stress, namely, 5 MN/m2 and 10 MN/m2.	Tensile properties of human articular cartilage from the femoral condyles of the knee deteriorated with increasing age.;
Athanasiou et al.	Inter-species comparison of mechanical properties	I	Tare load: 0.03-0.04 N / Preconditioning: Not reported / Test: 0.0980N for rabbit, monkey and canine. 0.1961 N for human and bovine. creep equilibrium time varied from 3000s to 10,800s (total 102 indentation tests)	Lateral condyle, aggregate modulus (human, n=4): 0.701 ± 0.228 MPa / Medial condyle, aggregate modulus (human, n=4): 0.588 ± 0.114 MPa / Patellar groove, aggregate modulus (human, n=4): 0.530 ± 0.094 MPa
Robinson et al.	Normal vs osteoarthritic (OA) cartilage	UC	Tare load: < 0.3 N tare load / Preconditioning: Not reported / Test: 30% strain at 20%/s	Young’s modulus of subchondral bone and calcified cartilage: / Tibia control: 447.1±218.7 MPa / Tibia OA: 375.5±371.7 MPa / Femur control:431.7±486.1 MPa / Femur OA: 469.2±438.7 MPa
Deneweth et al.	Tibial plateau heterogeneity	UC	Tare load: 0.2 N tare load / Preconditioning: 10 cycles at 100%/s to 20% strain / Test: 3 trials of 100%/s to 20% strain rapidly return to 0% strain. (~stance phase of gait)	tangent modulus to the stress–strain curve at 10% strain for various locations: 1-80 MPa
Korhonen et al.	Equilibrium response at confined, unconfined compression and indentation	CC, UC	Tare load: 12.5 kPa / Preconditioning: / Test: step-wise stress–relaxation tests (each step 5% strain at velocity 1 μm/s) up to a strain of 20%. Complete relaxation was a relaxation rate <100 Pa/min. (indentor diameter: 1mm, 3 mm)	Patella Young’s modulus, unconfined: 0.57±0.17 MPa (n=8, diameter= 3.7mm) / Femur Young’s modulus, unconfined: 0.31±0.18 MPa (n=9, diameter= 3.7mm ) / Patella aggregate modulus, confined: / 0.62±0.19 MPa (n=8, diameter= 3.7mm) Femur aggregate modulus, confined: 0.34±0.17 MPa (n=9,diameter= 3.7mm) / Patella Young’s modulus, indentation: / 0.83 ±70.21 MPa (n=8, diameter=1.0 mm) Femur Young’s modulus, indentation: 0.55 ±70.19 MPa (n=9,diameter= 1.0 mm)
Shepherd et al.	Instantaneous compressive modulus	I	Tare load: not reported / Preconditioning: not reported / Test: Cartilage loaded within 30 ms (compressed spring in apparatus applies the full load (10.5 N) in 10–15 ms), noted from referenced study.	Results for set 1 knee (out of 11 sets): / Compressive modulus: patellar surface: 5.9 (2.1) MPa, femur: 8.3 (4.2) MPa, covered tibial plateau: 5.9(2.3) MPa, direct tibial plateau: 2.8(0.5) MPa.
Nissi et al.	Estimation of mechanical properties using MRI	UC, MRI	Tare load: 10% pre-strain (MRI) / Preconditioning: not reported (MRI) / Test: UC: 10% strain with 2 mm/s ramp rate and 40 min of relaxation, dynamic response was measured using sinusoidal (1Hz) loading experiment. / MRI: Depth wise relaxation time profiles determined by averaging 3-pixel wide columns across cartilage depth.	Equilibrium modulus (Young’s modulus): 0.19 to 0.96 MPa (human samples) / Dynamic modulus: 0.85 to 8.43 MPa (human samples) / Note: significant negative correlation between equilibrium stiffness and T1 and T2 relaxation times in human samples. Significant positive correlation between T2 and dynamic stiffness.
Morel et al.	Study effects of injurious compression	UC	Tare load: not reported / Preconditioning: not reported / Test: Compression applied at 0.07/s and 0.00007/s up to 14 MPa. Note: on day 6, half the samples received 300 μm deep vertical slices	Swelling / change in thickness was significant between day 6 and 10 for sliced samples. Wet weight of unsliced samples remained the same.

References:

1.	Langelier, E. & Buschmann, M. D. Increasing strain and strain rate strengthen transient stiffness but weaken the response to subsequent compression for articular cartilage in unconfined compression. J Biomech 36, 853–859 (2003).
2.	Töyräs, J. et al. Estimation of the Young’s modulus of articular cartilage using an arthroscopic indentation instrument and ultrasonic measurement of tissue thickness. J Biomech 34, 251–256 (2001).
3.	Lai, J. H. & Levenston, M. E. Meniscus and cartilage exhibit distinct intra-tissue strain distributions under unconfined compression. Osteoarthr. Cartil. 18, 1291–1299 (2010).
4.	Boschetti, F., Pennati, G., Gervaso, F., Peretti, G. M. & Dubini, G. Biomechanical properties of human articular cartilage under compressive loads. Biorheology 41, 159–166 (2004).
5.	Jurvelin, J. S., Buschmann, M. D. & Hunziker, E. B. Mechanical anisotropy of the human knee articular cartilage in compression. Proc Inst Mech Eng H 217, 215–219 (2003).
6.	Treppo, S. et al. Comparison of biomechanical and biochemical properties of cartilage from human knee and ankle pairs. J. Orthop. Res. 18, 739–748 (2000).
7.	Armstrong, C. G. & Mow, V. C. Variations in the intrinsic mechanical properties of human articular cartilage with age, degeneration, and water content. J Bone Joint Surg Am 64, 88–94 (1982).
8.	Charlebois, M., McKee, M. D. & Buschmann, M. D. Nonlinear tensile properties of bovine articular cartilage and their variation with age and depth. J Biomech Eng 126, 129–137 (2004).
9.	Froimson, M. I., Ratcliffe, A., Gardner, T. R. & Mow, V. C. Differences in patellofemoral joint cartilage material properties and their significance to the etiology of cartilage surface fibrillation. Osteoarthritis and Cartilage 5, 377–386 (1997).
10.	Bellucci, G. & Seedhom, B. B. Mechanical behaviour of articular cartilage under tensile cyclic load. Rheumatology 40, 1337–1345 (2001).
11.	Gao, L.-L., Zhang, C.-Q., Gao, H., Liu, Z.-D. & Xiao, P.-P. Depth and rate dependent mechanical behaviors for articular cartilage: experiments and theoretical predictions. Mater Sci Eng C Mater Biol Appl 38, 244–251 (2014).
12.	Changoor, A., Fereydoonzad, L., Yaroshinsky, A. & Buschmann, M. D. Effects of refrigeration and freezing on the electromechanical and biomechanical properties of articular cartilage. J Biomech Eng 132, 064502 (2010).
13.	Thambyah, A., Nather, A. & Goh, J. Mechanical properties of articular cartilage covered by the meniscus. Osteoarthr. Cartil. 14, 580–588 (2006).
14.	Bursać, P. M., Obitz, T. W., Eisenberg, S. R. & Stamenović, D. Confined and unconfined stress relaxation of cartilage: appropriateness of a transversely isotropic analysis. Journal of Biomechanics 32, 1125–1130 (1999).
15.	Nguyen, A. M. & Levenston, M. E. Comparison of osmotic swelling influences on meniscal fibrocartilage and articular cartilage tissue mechanics in compression and shear. J. Orthop. Res. 30, 95–102 (2012).
16.	Kempson, G. E. Relationship between the tensile properties of articular cartilage from the human knee and age. Ann. Rheum. Dis. 41, 508–511 (1982).
17.	Athanasiou, K. A., Rosenwasser, M. P., Buckwalter, J. A., Malinin, T. I. & Mow, V. C. Interspecies comparisons of in situ intrinsic mechanical properties of distal femoral cartilage. J. Orthop. Res. 9, 330–340 (1991).
18.	Robinson, D. L. et al. Mechanical properties of normal and osteoarthritic human articular cartilage. J Mech Behav Biomed Mater 61, 96–109 (2016).
19.	Deneweth, J. M., Newman, K. E., Sylvia, S. M., McLean, S. G. & Arruda, E. M. Heterogeneity of tibial plateau cartilage in response to a physiological compressive strain rate. J. Orthop. Res. 31, 370–375 (2013).
20.	Korhonen, R. K. et al. Comparison of the equilibrium response of articular cartilage in unconfined compression, confined compression and indentation. Journal of Biomechanics 35, 903–909 (2002).
21.	Shepherd, D. E. & Seedhom, B. B. The ‘instantaneous’ compressive modulus of human articular cartilage in joints of the lower limb. Rheumatology (Oxford) 38, 124–132 (1999).
22.	Nissi, M. J. et al. Estimation of mechanical properties of articular cartilage with MRI - dGEMRIC, T2 and T1 imaging in different species with variable stages of maturation. Osteoarthr. Cartil. 15, 1141–1148 (2007).
23.	Morel, V., Berutto, C. & Quinn, T. M. Effects of damage in the articular surface on the cartilage response to injurious compression in vitro. J Biomech 39, 924–930 (2006).
Appendix B:

Table B1. Reference lengths for preconditioning and pre- and post- preconditioning ramps of repeated tests. SD: standard deviation
Test type	Location	Reference length, mm (mean, SD)
Uniaxial tension	Patella	7.88, 0.58
	Trochlear groove	6.96, 0.07
	Medial femoral condyle	7.04, 0.11
	Lateral femoral condyle	6.94, 0.23
	Medial tibial plateau	6.74, 0.15
	Lateral tibial plateau	6.91, 0.20

Appendix C:

Figure C1. Stress relaxation repeatability of all testing conditions for femoral condyle samples.

Figure C2. Stress relaxation repeatability of all testing conditions for tibial plateau samples.