Tables

Table 1. Detailed testing protocol for all test types with all parameters and justifications of why they were chosen. The development of protocols was motivated and guided by the goals of obtaining macro-scale specimen-specific and location dependent material properties, acquiring a variety of test information via different test types, limitations of the testing system, and keeping the parameters withing non-destructive physiological limits. The testing parameters were also chosen via experiential learning (e.g., number of freeze thaw cycles, number of preconditioning cycles etc.) All data were sampled at 2.5kHz.

Testing protocol	Parameters	Justification
1. Establish contact for compression / obtain reference length for uniaxial tension	10 g load at 0.005 mm/s / Filtered at 20Hz using a low pass Butterworth filter during the test.	Load is low enough so as to not strain the tissue out of the toe region. Filter was used to remove noise due to machine vibrations.
2. Ramp load - unload	15 % strain at 20 %/s strain rate followed by immediate unload at the same rate. (starting 300 µm offset from contact)	To obtain tissue response before preconditioning.
3. Preconditioning	1000 cycles between 10 and 15 % strain at 2Hz.(starting 300 µm offset from contact)	Cheng et al. 33suggests soft tissues should be preconditioned to the maximum strain used in the study, experiential learning from pilot tests (number of cycles gave repeatable results in pilot tests and 10-15 % strain avoided sample dislodging during unconfined compression test)
4. Ramp load - unload	15 % strain at 20 %/s strain rate followed by immediate unload at the same rate. (starting 300 µm offset from contact)	To obtain tissue response after preconditioning.
5. Establish contact for compression / obtain reference length for uniaxial tension	10 g load at 0.005 mm/s / Filtered at 20Hz using a low pass Butterworth filter during the test.	Load is low enough so as to not strain the tissue out of the toe region. Filter was used to remove noise due to machine vibrations.
6. Multi-step stress-relaxation	Ramp to 5-10-15% target strains at 20%/s strain rate and a 30 minutes wait (starting 300 µm offset from contact)	Multi-step test allows examination of a non-linear relaxation model at different strain levels. The strain and strain rates (while trying to reach as high as possible) were decided upon after pilot repeatability tests, assessing limits of testing system to apply them with accuracy and to stay within the non-destructive load ranges.

Table 2. Locations and dimensions of all samples based on test type for each repeatability set. Diameter for all confined and unconfined compression samples was assumed to be 5 mm based on the punch dimensions. Width for all tensile samples was assumed to be 1 mm based on punch dimensions. For tensile tests, the lengths are reference lengths obtained before stress – relaxation phase of repeated tests (lengths for preconditioning and pre and post preconditioning ramps are provided as supplementary material in Appendix B). Mean and standard deviation (SD) of thickness represent repeated measurements using the optical measurement system.

Test type	Location	Thickness, mm / (Mean, SD)	Length, mm / (Mean, SD)
Unconfined compression	Patella	2.68, 0.011	-
	Trochlear groove	1.40, 0.006	-
	Medial femoral condyle	1.83, 0.007	-
	Lateral femoral condyle	1.55, 0.013	-
	Medial tibial plateau	1.84, 0.002	-
	Lateral tibial plateau	2.26, 0.014	-
Confined / compression	Patella	2.68, 0.330	-
	Trochlear groove	1.42, 0.008	-
	Medial femoral condyle	1.84, 0.010	-
	Lateral femoral condyle	1.55, 0.004	-
	Medial tibial plateau	1.85, 0.004	-
	Lateral tibial plateau	2.25, 0.008	-
Uniaxial / tension	Patella	0.62, 0.036	8.24, 0.560
	Trochlear groove	0.79, 0.016	7.04, 0.050
	Medial femoral condyle	0.77, 0.062	7.14, 0.060
	Lateral femoral condyle	0.63, 0.068	7.13, 0.180
	Medial tibial plateau	0.69, 0.035	6.87, 0.080
	Lateral tibial plateau	1.03, 0.130	7.06, 0.078

Table 3. For full loading ramps (target strain of 15%), high strain modulus before and after preconditioning for all repeatability test sets. See manuscript text for description of high strain modulus calculation.

Test type	Location	High strain modulus before preconditioning, MPa / (Mean, SD)	High strain modulus after preconditioning, MPa / (Mean, SD)
Unconfined compression	Patella	2.75, 0.31	1.95, 0.10
	Trochlear groove	8.50, 0.99	4.42, 0.70
	Medial femoral condyle	21.40, 1.29	6.7, 4.11
	Lateral femoral condyle	17.44, 3.38	5.37, 0.64
	Medial tibial plateau	3.56, 0.73	1.73, 0.33
	Lateral tibial plateau	12.06, 1.38	6.00, 0.34
Confined / compression	Patella	16.45, 2.63	8.65, 1.33
	Trochlear groove	6.33, 1.94	4.87, 1.69
	Medial femoral condyle	17.38, 0.12	13.67, 1.02
	Lateral femoral condyle	12.96, 0.61	12.43, 1.80
	Medial tibial plateau	7.15, 0.43	4.67, 0.73
	Lateral tibial plateau	18.15, 0.33	12.35, 1.10
Uniaxial / tension	Patella	8.65, 2.49	9.34, 1.14
	Trochlear groove	47.94, 2.16	47.6, 0.41
	Medial femoral condyle	91.09, 6.15	92.72, 1.88
	Lateral femoral condyle	25.33, 3.08	26.62, 2.13
	Medial tibial plateau	35.31, 4.49	34.73, 2.92
	Lateral tibial plateau	40.87, 8.61	39.57, 6.82

Table 4. Percent stress reduction during preconditioning after 20 cycles and 1000 cycles of repeated tests. SD: standard deviation. For unconfined compression test for medial femoral condyle, the sample moved from it's original position and hence the percentage relaxation could not be accurately estimated as the forces dropped unexpectedly.

Test type	Location	% reduction after 20 cycles / (Mean, SD)	% reduction after 1000 cycles / (Mean, SD)
Unconfined compression	Patella	13.02, 0.64	49.44, 4.66
	Trochlear groove	27.16, 0.79	68.90, 0.40
	Medial femoral condyle	22.91, 1.05	82.65, 11.69
	Lateral femoral condyle	26.96, 2.90	79.40, 0.71
	Medial tibial plateau	18.32, 2.09	60.25, 5.98
	Lateral tibial plateau	16.20, 0.62	68.16, 3.14
Confined / compression	Patella	20.19, 0.23	64.43, 0.77
	Trochlear groove	21.51, 4.26	56.45, 3.18
	Medial femoral condyle	14.99, 1.20	68.28, 2.09
	Lateral femoral condyle	19.21, 2.16	66.59, 0.71
	Medial tibial plateau	13.36, 1.38	46.89, 0.35
	Lateral tibial plateau	11.99, 1.11	55.63, 1.45
Uniaxial / tension	Patella	11.36, 0.27	26.84, 1.77
	Trochlear groove	9.48, 1.32	25.73, 3.23
	Medial femoral condyle	7.48, 1.21	20.59, 3.39
	Lateral femoral condyle	12.32, 1.66	29.94, 2.98
	Medial tibial plateau	8.16, 1.53	21.38, 4.59
	Lateral tibial plateau	7.74, 2.26	22.05, 6.16

Table 5. Average instantaneous modulus (AIM) and average equilibrium modulus (AEM) calculated for all stress relaxation repeatability sets for each test type. Mean, standard deviations (SD) and coefficient of variation (COV) for each set are reported. See manuscript text for descriptions of AIM and AEM calculations.

Test type	Location	AIM, MPa / (Mean, SD)	AEM, MPa / (Mean, SD)	COV, AIM / (%)	COV, AEM / (%)
Unconfined compression	Patella	0.85, 0.092	0.19, 0.013	10.8	6.83
	Trochlear groove	1.91, 0.080	0.23, 0.014	4.39	6.03
	Medial femoral condyle	3.66, 0.070	0.199, 0.017	1.97	8.6
	Lateral femoral condyle	5.24, 1.140	0.22, 0.039	21.82	17.77
	Medial tibial plateau	2.57, 0.345	0.557, 0.083	13.43	15.032
	Lateral tibial plateau	2.34, 0.164	0.343, 0.015	6.98	4.39
Confined / compression	Patella	3.86, 0.26	0.26, 0.005	6.96	2.17
	Trochlear groove	3.60, 0.77	0.39, 0.560	21.58	14.19
	Medial femoral condyle	5.12, 0.115	0.287, 0.012	2.25	4.20
	Lateral femoral condyle	5.51, 0.209	0.237, 0.02	3.80	9.24
	Medial tibial plateau	3.09, 0.620	0.43, 0.119	20.25	27.32
	Lateral tibial plateau	5.05, 0.690	0.56, 0.076	13.82	13.54
Uniaxial / tension	Patella	6.24, 0.460	3.24, 0.380	7.46	11.77
	Trochlear groove	22.91, 0.970	14.23, 0.523	4.27	3.74
	Medial femoral condyle	48.39, 1.78	33.58, 0.560	3.69	1.68
	Lateral femoral condyle	13.23, 0.42	7.20, 0.522	3.18	7.25
	Medial tibial plateau	18.59, 0.24	12.89, 0.63	1.28	4.88
	Lateral tibial plateau	24.52, 0.44	18.14, 0.550	1.81	3.05

Table 6. High strain instantaneous modulus and high strain equilibrium modulus for each repeatability test set along with coefficients of variation (calculated using stress relaxation data). See manuscript text for descriptions of high strain moduli calculations.

Test type	Location	High strain instantaneous modulus, MPa / (Mean, SD)	High strain equilibrium modulus, MPa / (Mean, SD)	COV, high strain instantaneous modulus / (%)	COV, high strain equilibrium modulus / (%)
Unconfined compression	Patella	1.33, 0.076	0.28, 0.0024	10.80	6.83
	Trochlear groove	3.22, 0.062	0.39, 0.045	1.93	11.45
	Medial femoral condyle	4.81, 0.129	0.289,0.056	2.69	19.42
	Lateral femoral condyle	5.19, 0.850	0.051, 0.070	16.50	146.56
	Medial tibial plateau	3.19, 0.120	0.78, 0.028	4.05	3.69
	Lateral tibial plateau	3.60, 0.230	0.62, 0.007	6.45	1.23
Confined / compression	Patella	7.78, 0.430	0.282, 0.038	5.56	13.54
	Trochlear groove	4.08, 1.480	0.392, 0.090	36.23	22.91
	Medial femoral condyle	4.27, 0.270	0.32, 0.057	6.41	17.55
	Lateral femoral condyle	3.80, 0.264	0.062,0.092	6.96	148.23
	Medial tibial plateau	4.72, 0.210	0.64, 0.070	4.55	10.87
	Lateral tibial plateau	5.24, 0.066	0.55, 0.120	1.27	21.73
Uniaxial / tension	Patella	8.87, 1.390	4.18, 1.180	15.72	28.18
	Trochlear groove	33.34, 0.70	25.900	2.11	2.719
	Medial femoral condyle	72.70, 1.100	59.51, 2.208	1.51	3.711
	Lateral femoral condyle	17.03, 1.400	11.99, 1.8	8.27	15.04
	Medial tibial plateau	29.62, 1.090	23.25, 2.55	3.71	10.97
	Lateral tibial plateau	42.37, 1.09	32.76, 3.68	2.57	11.25

Table 7. Achieved strains after 10g digital load adjustment for each repeatability test set for stress relaxation. Low target strain was 5% (0.05), mid target strain was 10% (0.10) and high target strain was 15% (0.15) as per experimental reference location of 10g load. SD: standard deviation.

Test type	Location	low strain (Mean, SD)	Mid strain (Mean, SD)	High strain (Mean, SD)
Unconfined compression	Patella	0.0644, 0.0037	0.114, 0.0038	0.1644, 0.0038
	Trochlear groove	0.081, 0.0030	0.131, 0.0032	0.181, 0.0034
	Medial femoral condyle	0.059, 0.0050	0.109, 0.0055	0.159, 0.0055
	Lateral femoral condyle	0.065, 0.0040	0.1159, 0.004	0.1658, 0.0041
	Medial tibial plateau	0.071, 0.0150	0.121, 0.014	0.1711, 0.0149
	Lateral tibial plateau	0.074, 0.0035	0.124, 0.0036	0.174, 0.0036
Confined / compression	Patella	0.058, 0.0010	0.108, 0.001	0.158, 0.0010
	Trochlear groove	0.062, 0.0019	0.112, 0.0019	0.162, 0.0019
	Medial femoral condyle	0.077, 0.0019	0.127, 0.0019	0.177, 0.0018
	Lateral femoral condyle	0.074,0.0018	0.124, 0.0017	0.174,0.0016
	Medial tibial plateau	0.064, 0.002	0.1146, 0.0024	0.164, 0.0024
	Lateral tibial plateau	0.063, 0.001	0.113, 0.0019	0.163, 0.0019
Uniaxial / tension	Patella	0.066, 0.0032	0.116, 0.0032	0.166, 0.003
	Trochlear groove	0.061, 0.0007	0.111, 0.0007	0.161, 0.0007
	Medial femoral condyle	0.061, 0.0014	0.1119, 0.0014	0.1619, 0.0014
	Lateral femoral condyle	0.066, 0.0020	0.116, 0.002	0.166, 0.003
	Medial tibial plateau	0.064, 0.0008	0.114, 0.0009	0.164, 0.0009
	Lateral tibial plateau	0.062, 0.0007	0.1123, 0.0007	0.162, 0.0007

Table 8. Percentage reduction of stress at each strain level of stress relaxation after 30 minute hold for each repeatability set. SD: standard deviation.

Test type	Location	% relaxation at low target strain / (Mean, SD)	% relaxation at mid target strain / (Mean, SD)	% relaxation at high target strain / (Mean, SD)
Unconfined compression	Patella	81.18, 3.329	76.89, 1.23	77.836, 0.895
	Trochlear groove	94.16, 1.17	88.53, 0.21	88.12, 0.55
	Medial femoral condyle	97.44, 0.47	95.04, 0.138	94.60,0.44
	Lateral femoral condyle	92.25, 1.04	94.29, 0.83	95.81,0.174
	Medial tibial plateau	78.97, 4.63	79.67, 0.719	78.09, 0.824
	Lateral tibial plateau	92.43, 0.44	87.39, 0.44	85.35, 0.52
Confined / compression	Patella	76.36, 2.37	88.63, 0.51	93.47, 0.53
	Trochlear groove	88.91, 3.17	87.96, 3.75	88.42,
	Medial femoral condyle	97.13, 0.44	95.141, 0.47	94.51, 0.31
	Lateral femoral condyle	96.38, 0.152	95.29, 0.25	95.89, 0.384
	Medial tibial plateau	83.07, 1.74	85.49, 0.40	85.96, 1.18
	Lateral tibial plateau	88.01, 1.99	88.55, 1.06	88.83, 0.14
Uniaxial / tension	Patella	67.24, 4.49	47.37, 0.78	49.79, 2.78
	Trochlear groove	60.85, 2.25	49.06, 1.52	36.98, 0.78
	Medial femoral condyle	56.52, 1.44	40.35, 0.53	30.01, 1.75
	Lateral femoral condyle	74.44,0.904	55.83, 0.54	45.89, 2.51
	Medial tibial plateau	67.46, 2.79	40.50, 0.44	31.52, 3.16
	Lateral tibial plateau	53.77, 2.78	30.76, 0.79	26.50, 4.05