Title

Proposed Testing Suite for Characterization of Articular Cartilage with Documented Repeatability

Authors

Snehal Chokhandre1,2
Ahmet Erdemir1,2

Affiliations

1. Computational Biomodeling (CoBi) Core, Lerner Research Institute, Cleveland Clinic
2. Department of Biomedical Engineering, Lerner Research Institute, Cleveland Clinic

Abstract

Articular cartilage mechanics has been extensively studied. Various approaches have been taken for mechanical characterization of the tissue over the years. Hence, there exists a wide variation in the literature in the procedures utilized for said characterization. As per the author's knowledge, there are no studies done to assess the repeatability of these procedures. Studies also often have limited focus on why a particular testing protocol was used or how it was developed. This study aimed to propose a set of mechanical characterization protocols for articular cartilage and supported it with repeatability tests for assessment of the procedures.

Background & Summary

general overview of articular cartilage → composition, micro-structure etc
standard testing procedures
Introduction of mechanical characterization in literature
animal studies → motivation
human studies → motivation
material model development
physiological strain and strain rates
effects of freezing
variability in methodology
lack of repeatability information for procedures
goal: proposing a mechanical characterization suite for articular cartilage for human knee supported by repeatability data to support utility of proposed procedures and specifications.

Methods

Specimen information
sample preparation
testing equipment
thickness measurement
sample storage
test environment
testing protocol (evolution and justification for each step? )

Results

Instantaneous and equilibrium moduli (overall, high strain, low strain) → multiple tests → individual, average, SD
peak forces for multiple tests, individual, average, SD
to assess whether appropriate strains and strain rates applied → expected and applied strain and rates, also duration of each ramp
zero strain estimate may lead to application of more than 15 % strain (10g force used to establish contact and assumed zero strain location for subsequent strain application)

Discussion

How do the results compare to literature?
How does the proposed protocol compare to the literature?
Limitations → one specimen, one sample each from each location
future studies → multiple specimens, indentation vs unconfined compression
utility of data
protocol utility → extended to articular cartilage located at any joint, standardized testing protocol
limitation in protocol evaluation/evolution → limited number of samples were tested before making improvements to protocols ( eg. in most cases cartilage unconfined compression tests are the least challenging to reproduce, 1000 preconditioning cycles were used to improved cc repeatability etc )

average moduli
rmse for all
pre and post pc moduli
data fitting

further/ not in the scope of paper: data fitting, mri of samples and inverse FEA etc, additional samples from the same specimen, additional specimens.

Figures

1. Protocol illustration
2. unconfined compression – six locations, 3 tests each
3. confined compression - six locations, 3 tests each
4. uniaxial tension - six locations, 3 tests each

Figure legends

Tables

Average moduli (instantaneous and equilibrium)
high strain moduli (instantaneous and equilibrium)
low strain moduli (instantaneous and equilibrium)
Peak forces

Acknowledgements

Competing interests

References

1.	Lu, X. L. & Mow, V. C. Biomechanics of articular cartilage and determination of material properties. Med. Sci. Sports Exerc. 40, 193–199 (2008).
2.	Morel, V., Berutto, C. & Quinn, T. M. Effects of damage in the articular surface on the cartilage response to injurious compression in vitro. J. Biomech. 39, 924–930 (2006).
3.	Langelier, E. & Buschmann, M. D. Increasing strain and strain rate strengthen transient stiffness but weaken the response to subsequent compression for articular cartilage in unconfined compression. J. Biomech. 36, 853–859 (2003).
4.	Töyräs, J. et al. Estimation of the Young’s modulus of articular cartilage using an arthroscopic indentation instrument and ultrasonic measurement of tissue thickness. J. Biomech. 34, 251–256 (2001).
5.	Lai, J. H. & Levenston, M. E. Meniscus and cartilage exhibit distinct intra-tissue strain distributions under unconfined compression. Osteoarthritis Cartilage 18, 1291–1299 (2010).
6.	Boschetti, F., Pennati, G., Gervaso, F., Peretti, G. M. & Dubini, G. Biomechanical properties of human articular cartilage under compressive loads. Biorheology 41, 159–166 (2004).
7.	Jurvelin, J. S., Buschmann, M. D. & Hunziker, E. B. Mechanical anisotropy of the human knee articular cartilage in compression. Proc. Inst. Mech. Eng. [H] 217, 215–219 (2003).
8.	Treppo, S. et al. Comparison of biomechanical and biochemical properties of cartilage from human knee and ankle pairs. J. Orthop. Res. Off. Publ. Orthop. Res. Soc. 18, 739–748 (2000).
9.	Armstrong, C. G. & Mow, V. C. Variations in the intrinsic mechanical properties of human articular cartilage with age, degeneration, and water content. J. Bone Joint Surg. Am. 64, 88–94 (1982).
10.	Charlebois, M., McKee, M. D. & Buschmann, M. D. Nonlinear tensile properties of bovine articular cartilage and their variation with age and depth. J. Biomech. Eng. 126, 129–137 (2004).
11.	Froimson, M. I., Ratcliffe, A., Gardner, T. R. & Mow, V. C. Differences in patellofemoral joint cartilage material properties and their significance to the etiology of cartilage surface fibrillation. Osteoarthritis Cartilage 5, 377–386 (1997).
12.	Bellucci, G. & Seedhom, B. B. Mechanical behaviour of articular cartilage under tensile cyclic load. Rheumatol. Oxf. Engl. 40, 1337–1345 (2001).
13.	Gao, L.-L., Zhang, C.-Q., Gao, H., Liu, Z.-D. & Xiao, P.-P. Depth and rate dependent mechanical behaviors for articular cartilage: experiments and theoretical predictions. Mater. Sci. Eng. C Mater. Biol. Appl. 38, 244–251 (2014).
14.	Changoor, A., Fereydoonzad, L., Yaroshinsky, A. & Buschmann, M. D. Effects of refrigeration and freezing on the electromechanical and biomechanical properties of articular cartilage. J. Biomech. Eng. 132, 064502 (2010).
15.	Thambyah, A., Nather, A. & Goh, J. Mechanical properties of articular cartilage covered by the meniscus. Osteoarthritis Cartilage 14, 580–588 (2006).
16.	Bursać, P. M., Obitz, T. W., Eisenberg, S. R. & Stamenović, D. Confined and unconfined stress relaxation of cartilage: appropriateness of a transversely isotropic analysis. J. Biomech. 32, 1125–1130 (1999).
17.	Nguyen, A. M. & Levenston, M. E. Comparison of osmotic swelling influences on meniscal fibrocartilage and articular cartilage tissue mechanics in compression and shear. J. Orthop. Res. Off. Publ. Orthop. Res. Soc. 30, 95–102 (2012).
18.	Kempson, G. E. Relationship between the tensile properties of articular cartilage from the human knee and age. Ann. Rheum. Dis. 41, 508–511 (1982).
19.	Athanasiou, K. A., Rosenwasser, M. P., Buckwalter, J. A., Malinin, T. I. & Mow, V. C. Interspecies comparisons of in situ intrinsic mechanical properties of distal femoral cartilage. J. Orthop. Res. Off. Publ. Orthop. Res. Soc. 9, 330–340 (1991).
20.	Robinson, D. L. et al. Mechanical properties of normal and osteoarthritic human articular cartilage. J. Mech. Behav. Biomed. Mater. 61, 96–109 (2016).
21.	Deneweth, J. M., Newman, K. E., Sylvia, S. M., McLean, S. G. & Arruda, E. M. Heterogeneity of tibial plateau cartilage in response to a physiological compressive strain rate. J. Orthop. Res. Off. Publ. Orthop. Res. Soc. 31, 370–375 (2013).
22.	Korhonen, R. K. et al. Comparison of the equilibrium response of articular cartilage in unconfined compression, confined compression and indentation. J. Biomech. 35, 903–909 (2002).
23.	Shepherd, D. E. & Seedhom, B. B. The ‘instantaneous’ compressive modulus of human articular cartilage in joints of the lower limb. Rheumatol. Oxf. Engl. 38, 124–132 (1999).
24.	Nissi, M. J. et al. Estimation of mechanical properties of articular cartilage with MRI – dGEMRIC, T2 and T1 imaging in different species with variable stages of maturation. Osteoarthritis Cartilage 15, 1141–1148 (2007).

Data citations

All data and codes disseminated publicly →