Protocol illustration:

Table 1: Specimen information
Study	Goal	Specimen source	Specimen age / and/or gender, BMI	# of specimens and samples	Sample location	Sample dimensions, how are they measured
Morel et al, 2005 2	Effects of injurious compression	Bovine	18 month old	Samples = 55 / Specimens = 1	Humeral heads	4mm diameter bone, 2.7 mm diameter cart plugs, full thickness / Measured using: microscope
Langelier et. al., 3	Assess strain and strain rate dependent stiffening	Bovine	1-2 yr old	4 discs /speed	Humeral heads	3 mm disc, varying thickness (<1mm) / Measured using:
Toyras et. al., 4	Determine Young's modulus and thickness	Bovine	-	7	Humeral heads	For unconfined compression – 3 mm diameter / Measured using:
Lai et. al., 5	Investigate depth varying compressive strains	Bovine	Young	72 total samples	Tibial articular cartilage	4 mm diameter / 1500 micron thick (bottom removed)
Boschetti et. al., 6	Properties of cartilage under compression	Human	73-M, 75-M, 81-F	3 specimens, 33 discs total	Femoral head	5 mm diameter, 650 micron thick, 3 layers
Jurvelin et; al., 7	Mechanical anisotropy or knee cartilage	Human	3 females, 7 males,	10 specimens	Patellofemoral groove	1.7 mm diameter, 1 mm thick
Treppo et. al., 8	Biomechanical comparison of knee-ankle cartilage pair	Human	-	8 specimens, 10 samples from each joint	Tibiofemoral, patellofemoral surfaces	3 mm disc , top 1mm slices
Armstrong et. al., 9	Variation in properties with age, water content, degeneration	Human	56.4 yrs (SD: 19.13)	103 samples	Patella	6.35 mm diameter
Charlebois et al., 10	Age and depth dependent tensile properties	Bovine	< 12 months - adult	26 specimens	Humeral heads	6-8 mm wide, 2 cm long, ~ 5 mm thick
Froimson et al., 11	Cartilage surface fibrilation effects	Human	18-41 yrs	17 specimens, / 10 sites each	Patellofemoral joint	1.5 mm dia indentor
Bellucchi et al., 12	Articular cartilage under tensile load	Human	48 yrs	1 specimen, 16 samples, 72 tensile specimens	Patellofemoral and tibiofemoral joints	0.2 mm thick, 1mm by 9 mm, multiple depths
Gao et al., 13	Depth and rate dependent cartilage behavior	Porcine	8 months	18 samples	trochlea sites of three joints of knee	5.5 by 4 mm, 2 mm thick
Changoor et al., 14	Effects of freezing	Bovine	~ 6 months	8 sites/ 4 samples each	Knee joint	3 mm diameter
Thambyah et al., 15	Properties of cartilage covered by meniscus	Human	62-70 yrs	7 specimens	Tibial plateau	Load bearing and non load bearing regions
Bursac et al., 16	Assess confined and unconfined stress relaxation with transversely isotropic model	Bovine	3-4 weeks old	3 specimens	Patellar groove	4.5 mm diameter, 3.5 mm thick
Nguyen et al., 17	Swelling influences on mechanics in compression and shear	Bovine	Immature	50 samples	Femoral condyles	4mm diameter, 2 mm thick mid-substance
G. E. Kempson 18	Relationship between tensile properties and age	Human	8-91 yrs	-	Femoral condyles	3 mm by 0.5 mm, 200 micron thick
Athanasiou et al., 19	Interspecies comparison of mechanical properties	Human and other	-	4 specimens	Distal femoral cartilage	1.5 mm diameter indentor
Robinson et al., 20	Normal vs osteoarthitic (OA) cartilage	Human	10 specimens OA (4 male,6 female, 69.7± 9.3 yrs ) , 3 specimens normal (1 male, 2 female, 59.1 ±7.2 yrs )	51 samples OA, / 43 sample normal	Tibiofemoral joint	3 mm diameter osteochondral plugs
Deneweth et al., 21	Tibial plateau heterogeneity	Human	All female , 18-55 yrs	8 specimens	Tibial plateau	4 mm diameter
Korhonen et al., 22	Equlibrium response at confined, unconfined compression and indentation	Bovine	-	26 samples	Humeral head	3.7 mm diameter for compression
Shepherd et al., 23	Instantaneous compressive modulus	Human	65.1 (14.3) yrs. 3 male , 8 female	11 specimens	Tibiofemoral joint	1.58 mm diameter
Nissi et al., 24	Estimation of mechanical properties using MRI	Human and other	24-78 yrs	12 specimens	Tibiofemoral joint	5 mm diameter

Table 2: sample preparation and testing details

Study	Goal	Sample preparation / (Previously frozen, hydrated, temperature, stabilized before testing)	Test type	Protocol (Tare load, preconditioning, test)	Output/ results/ material properties	Material property calculation
Morel et al, 2005 2	Effects of injurious compression	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization: incubated for several days	Unconfined Compression	Tare load: / Preconditioning: / Test: Compression applied at 0.07/s and 0.00007/s upto 14 Mpa.	Swelling / thickness	N/A
Langelier et. al., 3	Assess strain and strain rate dependent stiffening	Previously frozen: / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	6g tare load, compression-hold-release (12.5; 25; 50; 100; 150; 200; 250; 300 mm) using 1 of 3 ramp speeds (0.5; 5; 50 mm/s	equilibrium stiffness of the first test ramp (12.5 mm) : 0.40– 0.61 MPa for low strain rate compression, 0.30– 0.56 MPa for moderate strain rate (fresh and frozen specimens) compression and 0.33–0.56 MPa for high strain rate compression.
Toyras et. al., 4	Determine Young's modulus and thickness	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Ultrasound, indentation and unconfined compression	Unconfined compression – stepwise stress relaxation.5 steps, each 4% of cartilage thickness, speed 2 mm/s ,relaxation time of 13 min between each step. The equilibrium stress-strain data in the linear range during the three last steps used to determine the equilibrium Young’s modulus	Young's modulus : 0.1- 1.6 MPa
Lai et. al., 5	Investigate depth varying compressive strains	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	compressed at 1 mm/s to 5, 10, 15, and 20% strain, relax for 20 min at each offset.	Average equilibrium compressive modulus: 0.447 (0.363, 0.531) MPa
Boschetti et. al., 6	Properties of cartilage under compression	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Confined and unconfined compression	1.5 MPa for 1800s	Confined : Average aggregate modulus: 0.25, 0.38,0.5 MPa. / Unconfined : Average Equilibrium modulus: 0.24, 0.38,0.5 MPa
Jurvelin et; al., 7	Mechanical anisotropy or knee cartilage	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Confined and unconfined compression	1 micron, 1 micron/s up to 20 % strain. Relaxation limit: 0.1g /min	Aggregate modulus: 0.845±0.383 MPa / Young's modulus: 0.581±0.168 MPa
Treppo et. al., 8	Biomechanical comparison of knee-ankle cartilage pair	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Confined compression	Static compressive strain 5-10% up to 25 %	Femur (n=48): Average aggregate modulus = ~ 0.6 MPa, Tibial plateau (n=31): ~ 0.5 MPa
Armstrong et. al., 9	Variation in properties with age, water content, degeneration	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Creep confined compression	0.1 MPa constant stress	Modulus: 0.79 MPa (0.36 )
Charlebois et al., 10	Age and depth dependent tensile properties	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Tensile	5 ramp of 2% strain up to 80 microns( 6 micron/second) . 48 hour long tests	modulus for the last step : 10.1 (3.3) MPa for young, 18.7(5.9) MPa for adolescent, and 28.3(16.6) MPa for adult.
Froimson et al., 11	Cartilage surface fibrilation effects	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Biphasic indentation	- --	Average aggregate modulus: 0.42 MPa (Patella) / 0.6 MPa (groove)
Bellucchi et al., 12	Articular cartilage under tensile load	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Cyclic Tensile	1.5 – 3 MPa maximum stress	Cycles to failure : 20 – 1.5 * 10^6
Gao et al., 13	Depth and rate dependent cartilage behavior	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression creep	stress rates0.0045, 0.045, 0.225 Mpa/s, constant compressive stress levels of 0.1, 0.5 and 1 MPa , creep time: 60 min	Young's modulus: / at 0.0045 MPa /s: 1.4-4.8 MPa (superficial – deep layer) / at 0.045 MPa /s: 5-6.5 MPa (superficial – deep layer)
Changoor et al., 14	Effects of freezing	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	ramps of 2% strain applied at a rate of 0.4% strain/s, relax until the load decay was 0.01 g/min	Fresh/ non frozen samples: fibril modulus, day 1: average 16.5 MPa (n=8) / matrix modulus, day 1: Average 0.7 MPa (n=8)
Thambyah et al., 15	Properties of cartilage covered by meniscus	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	indentation	axial compression at a constant load of 0.5 N (0.6 MPa ), with the use of a 1-mm diameter indenter, 60s hold.	Lat plateau not covered by meniscus: 2.13 (0.74) MPa / Med plateau not covered by meniscus: 3.51 (1.42) MPa / Lat plateau covered by meniscus: 3.77 (1.25) MPa / Med plateau covered by meniscus: 5.13 (1.91) MPa
Bursac et al., 16	Assess confined and unconfined stress relaxation with transversely isotropic model	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Confined and unconfined compression	Steps of 3% ramp up to 15 % strain (0.115 micron /s )	Aggregate modulus, MPa at 6%,9%,12%,15% strain: 1.72 (0.72), 1.23 (0.4), 0.97 (0.2), 0.79 (0.12). / Young's modulus, MPa at 6%,9%,12%,15% strain: 1.5 (0.5), 1.09 (0.43), 0.74 (0.28), 0.68 (0.13).
Nguyen et al., 17	Swelling influences on mechanics in compression and shear	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	5%, 10%, 15%, and 20% strain at 0.1%/s, 20 min relaxation	1.47 ± 0.13 MPa
G. E. Kempson 18	Relationship between tensile properties and age	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Tensile test	( Protocol unclear) tensile stiffness determined from the gradient to the stress strain curve at 2 levels of stress, namely, 5 MN/m2 and 10 MN/m2.	Tensile properties of human articular cartilage from the femoral condyles of the knee deteriorated with increasing age
Athanasiou et al., 19	Interspecies comparison of mechanical properties	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Indentation	Tare load (0.03-0.04 N), 0.1961 N load, 3 hour creep relaxation	Lateral condyle, modulus= 0.701 ± 0.228 MPa / Medial condyle, modulus: 0.588 ± 0.114 MPa / Patellar groove, modulus: 0.530 ± 0.094 MPa
Robinson et al., 20	Normal vs osteoarthitic (OA) cartilage	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	< 0.3 N tare load, 30% strain at 20%/s (estimated walking rate)	Tibia control: 447.1±218.7 MPa / Tibia OA: 375.5±371.7 MPa / Femur control:431.7±486.1 MPa / Femur OA: 469.2±438.7 MPa
Deneweth et al., 21	Tibial plateau heterogeneity	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	0.2 N tare load, 10 cycles at 100%/s to 20% strain. 3 trials of 100%/s to 20% strain rapidly return to 0% strain. (~ stance phase of gait )	tangent modulus to the stress–strain curve at 10% strain for various locations: 1-80 MPa
Korhonen et al., 22	Equlibrium response at confined, unconfined compression and indentation	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Confined and unconfined compression	stepwise stress–relaxation tests (each step 5% strain at velocity 1 mm/s) up to a strain of 20%. Complete relaxation was a relaxation rate <100 Pa/min.	Patella modulus, unconfined : 0.57±0.17 MPa / Femur modulus, unconfined: 0.31±0.18 MPa / Patella modulus, confined : / 0.62±0.19 MPa Femur modulus, confined: 0.34±0.17 MPa
Shepherd et al., 23	Instantaneous compressive modulus	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Indentation	Cartilage loaded within 30 ms (compressed spring in apparatus applies the full load (10.5 N) in 10–15 ms.)	Sample set: / Compressive modulus, patella: 5.9 (2.1) MPa. / Femur: 8.3 (4.2) MPa
Nissi et al., 24	Estimation of mechanical properties using MRI	Previously frozen: No / Hydrated: / Hydration source: / Temperature: / Stabilization:	Unconfined compression	Compression: 10% prestrain, 10% strain with 2 mm/s ramp rate and 40 min of relaxation	Equilibrium modulus (Young’s modulus): 0.19 to 0.96 MPa